5XXXXX

| APPLICATION | REVISIONS |
| --- | --- |
| NEXT ASSY | USED ON | LTR | DESCRIPTION | DATE (YY-MM-DD) | APPROVED |
|  | 06250000 | ( | RELEASED PER ERN |  |  |
|  | 06290000 |  |  |  |  |
|  | 06140000 |  |  |  |  |
| ALTERED ITEM DRAWING |
| ALL SHEETS ARE THE SAME REVISION |
| UNLESS OTHERWISE SPECIFIED DIMENSIONS ARE IN INCHES AND INCLUDE CHEMICALLY APPLIED OR PLATED FINISHES DO NOT SCALE PRINT TOLERANCES | CONTRACT NO. General |  |
|  | APPROVALS |  |
|  | DRAWN | D. Wages |  |
|  | CHECKED |  |  |
|  | ENGINEER | G. Richards |  |
| DECIMALS | ANGLE |  |  |  |  |
|  |  | OTHER |  |  |  |
| 2 PLACE | 3 PLACE |  |  |  |  |  |
| (0.02 | (0.015 | ±2( |  |  |  |  |

- SCOPE

  - Scope.  This specification defines the requirements for solder dipping of terminal lugs.

- APPLICABLE DOCUMENTS

## Issues of Documents.  The following documents of the issue in effect on the date of solicitation form a part of this specification to the extent specified herein.

## Order of Precedence.  In the event of conflict between the requirements of this specification and those listed, the requirements of this specification shall govern.

SPECIFICATIONS

Military

MS77067	Terminal, Lug, Solder Type, Phosphor Bronze Stamping Locking Type, Flat, One Hole

MS77068	Terminal, Lug, Solder Type, Phosphor Bronze Stamping Locking Type, 45 Deg., Two Hole

Industry

NASM77072	Terminal, Lug, Solder Type, Phosphor Bronze Stamping Locking Type, Flat, One Hole

ASME-Y14.5M	Dimensioning and Tolerancing

.

- REQUIREMENTS

  - Terminals listed in Table 1 shall be soldered dipped per the following procedure:

    - Record original manufacturer name, part number, and lot code on traveler.

    - Clean terminals with suitable agent to remove corrosion, dirt, and other contaminants.

    - Solder dip terminals using either Sn63/Pb37 or Sn60/Pb40 solder.  The entire surface of the terminal shall be completely covered with solder to a minimum thickness of 50 micro-inches.

3.1.3.1	Solder used for dipping shall be replaced at regular intervals to assure that contamination is minimized. The tin content shall be maintained within ±1% of the nominal alloy being used.

    - Clean terminals with suitable agent to remove flux and other contaminants.

    - Perform solderability test in accordance with Mil-Std-202, Method 208 or J-Std-002. Sample size shall be a 1% AQL.

  - Workmanship

Workmanship shall be in accordance with Mil-T15659

  - Marking

Marking shall be bag and tag.  Re-identify terminals passing all tests with the applicable part number of Table 1. Retain manufacturer original part number and lot date code.

- QUALITY ASSURANCE PROVISIONS

  - Lugs shall meet the quality assurance requirements of Mil-T-15659

  - Acceptance inspection shall consist of verifying workmanship, plating thickness/composition, physical dimensions, cleanliness and solderability. Sample size is 1% AQL.

- PREPARATION FOR DELIVERY

  - Packaging.  The preparation for delivery, packaging, preservation and handling shall be in accordance with MIL-T-15659.

  - Documentation.

Documentation provided with shipment shall include:

Certificate of conformance

Lot traveler

Inspection Attributes Data

Certificate of plating composition

- NOTES

  - Approved Source(s) of Supply.  Only the item(s) described on this drawing when procured from the vendor(s) listed herein, is approved by the Buyer for use in the application(s) specified herein.  A substitute item shall not be used without the written approval by the Buyer.

  - Suggested Source(s) of Supply.  Identification of the suggested source(s) of supply hereon is not to be construed as a guarantee of present or continued availability as a source of supply for the item(s).

| (A) | Hardware Specialty Company | (B) | Zeirick Manufacturing Corp |
| --- | --- | --- | --- |
|  | 3419 11th Ave SW |  | 131 Radio Circle |
|  | Seattle, Washington 98134-1007 |  | Mount Kisco, New York |
|  | CAGE: 54517 |  | CAGE: 79963 |

  - Dimensioning and Tolerancing.  Dimensioning and tolerancing in accordance with ASME-Y14.5M.

Table 1. Altered Item Cross Reference

| IDENTIFYING PART NO. | MAKE FROM PART NUMBER | FIGURE |
| --- | --- | --- |
| 8227615-1 | MS77067-1 | 1 |
| 8227615-2 | MS77067-2 | 1 |
| 8227615-3 | MS77067-3 | 1 |
| 8227615-4 | MS77068-1 | 2 |
| 8227615-5 | MS77068-2 | 2 |
| 8227615-6 | MS77068-3 | 2 |
| 8227615-7 | MS77068-4 | 2 |
| 8227615-8 | MS77072-1 | 3 |
| 8227615-9 | MS77072-2 | 3 |
| 8227615-10 | MS77072-3 | 3 |
| 8227615-11 | MS77072-4 | 3 |

Material thickness is 0.018± 0.003

| Part Number | Screw Size | Hole Dia A minimum | Hole Dia A maximum |
| --- | --- | --- | --- |
| 8227615-1 | 4 | 0.115 (2.92) | 0.127(3.26) |
| 8227615-2 | 6 | 0.141(3.58) | 0.153(3.89) |
| 8227615-3 | 8 | 0.167(4.24) | 0.179(4.55) |

Figure 1. MS77067 type

Material thickness is 0.018± 0.003

| Part Number | Screw Size | Hole Dia A minimum | Hole Dia A maximum |
| --- | --- | --- | --- |
| 8227615-4 | 4 | 0.115 (2.92) | 0.127(3.26) |
| 8227615-5 | 6 | 0.141(3.58) | 0.153(3.89) |
| 8227615-6 | 8 | 0.167(4.24) | 0.179(4.55) |
| 8227615-7 | 10 | 0.193(4.90) | 0.205(5.21) |

Figure 2. MS77068 type

Material thickness is 0.018± 0.003

| Part Number | Screw Size | Hole Dia A minimum | Hole Dia A maximum |
| --- | --- | --- | --- |
| 8227615-8 | 4 | 0.115 (2.92) | 0.127(3.26) |
| 8227615-9 | 6 | 0.141(3.58) | 0.153(3.89) |
| 8227615-10 1/ 2/ | 6 | 0.141(3.58) | 0.153(3.89) |
| 8227615-11 | 8 | 0.167(4.24) | 0.179(4.55) |

Notes:

1/ For 8227615-10, dimension is 0.250±0.015 (6.35±0.38)

2/ For 8227615-10, dimension is 0.078 (1.98)

Figure 3. MS77072 type

THIS IS THE LAST PAGE OF THIS DOCUMENT

# Text boxes

2/

1/